## Slide 1: Corrosion of Roofing Fastener Systems
Interim Report
March 2, 2016
Kurtis Gurley, PhD, Forrest Masters, PhD, PE
Associate Professor of Civil Engineering
Engineering School of Sustainable Infrastructure & Environment
University of Florida

## Slide 2: Background
2013 – 2014: Survey of 385 roofing contractors
  Electrogalvanized fastener corrosion is common
  Corrosion in coastal applications is prevalent
  Corrosion in inland applications is not uncommon
  Outcomes justified a follow up experimental studies
2014 – 2015: Experimental evaluation of fastener corrosion
  Electrogalvanized fasteners tested in multiple configurations
  Applied TAS 114 Appendix E test protocol
  Gradations of corrosion documented

## Slide 3: Testing: 2014 - 2015
Test out-of-the-box fasteners side-by-side with fasteners installed / removed in various substrates
The test protocol followed TAS 114 Appendix E
  Failure if > 5% surface area indicates failure
An integer scale of 1 – 8 was created to classify the degree of corrosion observed on the fasteners

## Slide 4
1: no corrosion observed
2: Edge corrosion only

## Slide 5
3: Light partial surface corrosion
most scores of 3 would fail TAS criterion of > 5% surface corrosion
4: Light full surface corrosion

## Slide 6
5: Partial heavy surface corrosion
6: Partial heavy and partial light full surface corrosion

## Slide 7
7: Heavy full surface corrosion without scaling
8: Heavy full surface corrosion with scaling

## Slide 8: Results: 2014 - 2015
Corrosion scale results for 16 roof fasteners tested out of the box (configuration OB)
Manufacturers C & D clearly shows better performance
This set corresponds to the TAS 114 test specimen conditions

## Slide 9: Results: 2014 - 2015
A wide disparity in the performance of electrogalvanized fasteners from different manufacturers was observed
A high failure rate of the TAS 114 criterion for electrogalvanized fasteners was observed
The tested fasteners were electrogalvanized, but not marked at ASTM A641 or TAS 114 compliant
The results provide a baseline against which to measure ASTM A641 and TAS 114 compliant fasteners
Are they any better than unlabeled EG fasteners?

## Slide 10: 2015 – 2016 Work
Goal: Determine whether ASTM A641 and TAS 114 Appendix E certified fastener performance exceeds the baseline electrogalvanized results from the 2014 – 2015 study
Approach: Apply TAS 114 Appendix E testing (Section 2.6.1) to evaluate the degree of corrosion resistance of ASTM A641 Class 1 fasteners and TAS 114 Appendix E certified fasteners

## Slide 11: 2015 – 2016 Work
Working with Mark Zehnal to identify and procure test specimens
  1 ¼” EG nails, HVHZ and non-HVHZ CHINA
  1 ¼” hot dipped coil nails CHINA
    Note: hot dipped coating ~ 10 times thicker zinc coating than EG
  3” stainless steel patio/deck nails TAIWAN
  2 ½” Electroplated (EP) tile screws USA
  2 ½” Mechanically galvanized tile screws USA
    Note mechanically galvanized thicker zinc coating than electroplated
  Hot dipped screws CHINA
Suppliers include north, central and south Florida
10 of each type were tested

## Slide 12: 2015 – 2016 Work
Table 1: 16 specimen types tested to date (10 samples of each) |  |  |  | 
Group number | Product type | Coating type | Certification | Supplier location
1 | 1 ¼ nail | EG | ASTM F1667 | Orlando
2 | 1 ¼ nail | EG | Unknown | Orlando
3 | 1 ¼ coil nail | EG | Unknown | Orlando
4 | 1 ¼ coil nail | EG | ASTM F1667 | Gainesville
5 | 1 ¼ coil nail | EG | ASTM A153 Class D | Orlando
6 | #8 2 ½ tile screw | MG | ASTM B695 Class 55 2006 IRC Compliant | Orlando
7 | #8 2 ½ tile screw | EP | unknown | Bradenton
8 | 1 ¼ coil nail | EG | ASTM F1667 | Bradenton
9 | 1 ¼ coil nail | HD | Unknown | Sarasota
10 | 1 ½ screws | HD | No info | No info
11 | 10d 3” RS | SS | MDC Approved HVHZ | Miami
12 | 1 ¼ RS nail | HD | MDC Approved ASTM F1667 HVHZ | Miami
13 | 1 ¼ nail | EG | MDC Approved ASTM F1667 HVHZ | Miami
14 | 1 ¼ coil RS nail | EG | MDC Approved ASTM A641 | Miami
15 | 1 ¼ coil RS nail | EG | Non HVHZ, MDC approved ASTM A641 | West Palm
16 | #8 2 ½ tile screw | MG | ASTM B695 Class 55 2006 IRC Compliant | West Palm
Notes: ASTM F1667  ASTM A641 compliant ASTM A153 Class D thicker zinc coating that ASTM A641 ASTM B695  mechanical galvanizing standard, Class 55  0.0022” zinc thickness HVHZ  Miami Dade County compliant EG  electrogalvanized, EP  electroplated, MG  mechanically galvanized, HD  hot dipped, SS  stainless steel |  |  |  | 

## Slide 13: 2015 – 2016 Work
Figure 1: All 1 ¼” electrogalvanized (EG) nails compliant with ASTM A641, non-HVHZ. Head results shown, shaft very similar
Generally, no improvement from
2014-2015 EG samples
Next graph: EG HVHZ

## Slide 14: 2015 – 2016 Work
Figure 2: All 1 ¼” EG nails compliant with ASTM A641, HVHZ approved. Head results shown, shaft very similar
HVHZ approved EG no better than
Non-HVHZ EG
Next graph: MG and EP tile screws

## Slide 15: 2015 – 2016 Work
Figure 3: #8 2 ½” roof tile screws, two mechanically galvanized specimens and one electroplated specimen. Head and shaft identical.
No visible corrosion on any
sample of MG tile screws
Next graph: Hot dipped and SS

## Slide 16: 2015 – 2016 Work
Figure 4: Two hot dipped 1 ¼” nail specimens, one hot dipped 1 ½” screw enclosure fastener specimen, and one 10d 3” stainless steel patio/deck nail specimen. Head results shown. Shaft results identical.
No visible corrosion on any
sample of hot dipped fasteners

## Slide 17: North Florida EG coil nail ASTM F1667  ASTM A641

## Slide 18: North Florida EG coil nail ASTM A153 class D > ASTM A641

## Slide 19: Central Florida EG coil nail ASTM F1667  ASTM A641

## Slide 20: South Florida EG coil nail ASTM A641 HVHZ – Approved

## Slide 21: Hot dipped nails

## Slide 22: Central Florida hot dipped screws

## Slide 23: North & South Florida mechanically galvanized tile screw

## Slide 24: Central Florida electroplated tile screw

## Slide 25: Stainless steel patio/deck nails

## Slide 26: 2015 – 2016 Work
Observations
  ASTM A641 certified EG performance no better than unlabeled EG fasteners from the previous year’s study
  HVHZ compliant EG fasteners (presumed TAS 114 E compliant) perform no better than non-HVHZ ASTM A641
  Hot dipped fasteners perform much better than EG fasteners
  Mechanically galvanized (MG) screws perform better than EP screws

## Slide 27: 2015 – 2016 Work
Observations
  Miami-Dade approved EG fasteners: The results thus far did not reveal a single EG sample that passed the TAS 114E criterion of < 5% surface corrosion. Each of the 30 such fastener samples tested had a score of at least 3 (partial light surface corrosion) on both the head and shaft, and most samples displayed significant heavy corrosion
    Requiring Miami-Dade approval for all EG fasteners used in Florida is not a viable code modification
  To date, among all 244 samples tested (88 in phase 2, 160 in phase 3), only the hot dipped and mechanically galvanized specimens demonstrated no corrosion in any of the samples (30 hot dipped, 20 mechanically galvanized samples)

## Slide 28: 2015 – 2016 Work
Upcoming work
  Procurement and testing of additional specimens
    EG ASTM A641 and Miami-Dade approved
    Seeking USA made 1 ¼” nail products
  Testing installed/removed hot dipped specimens to investigate the suggestion that hot dipped treatment is more brittle than EG (FRSA member suggestion)